Sutper®TPE R1010008

Product Description

A soft, colorable SBS-based thermoplastic elastomer (TPE) compound. The product has uniform particle size and is free of impurities, offering excellent physical properties and chemical resistance.

| Specifications |  |  |  |
| --- | --- | --- | --- |
| Applications | •single-component injection molding handle material |  |  |
| Environmental | •RoHS compliant |  |  |
| Appearance | •white color |  |  |
| Form | •Granules |  |  |
| Molding method | •Injection molding |  |  |
| Availability | •Europe •North America •Asia •Africa & Middle East |  |  |
| Physical Properties Typical Value Unit Test Method |  |  |  |
| Density Melt Flow Index (190℃*2.16kg) | 1.1 40 | g/cm3 g/10min | ASTM D792 ASTM D1238 |
| Hardness Typical Value Unit Test Method |  |  |  |
| Shore A,10sec,23℃ | 60 | A | ASTM D2240 |
| Mechanical Properties Typical Value Unit Test Method |  |  |  |
| 100% Tensile Strength - vertical flow (23°C) | 1 | Mpa | ASTM D412 |
| Tensile Strength - Vertical Flow (23°C) | 2 | Mpa | ASTM D412 |
| Break Elongation-Vertical Flow23℃ | 500 | % | ASTM D412 |
| Tear Strength -Vertical Flow 23℃ Die C | 10 | KN/m | ASTM D624 |
| Additional Information |  |  |  |
| - The above test data were obtained using fan gate injection molded specimens with dimensions of 110 mm × 80 mm × 2 mm. The tensile strength, elongation at break, and stress at a given elongation were tested perpendicular to the flow direction, while tear strength was tested along the flow direction. - The properties listed are typical and should not be considered technical specifications or part of an agreement. - The user should be aware that Sutper needs to confirm all final details before taking any action based on the information and recommendations in this document. |  |  |  |